Veneering Notes

November 10, 2012

Commercial Veneer Thickness

- Pre 1996 -- 1/28 (.035)

- Post 1996 -- 1/40 (.025) ----1/60  (.017)

Flattening Veneer

- Glue Sizing –

  - 1 part hide glue, 5-8 parts water.  Heat to 140 degrees before use.  Use hot or cold.  Dispose after 5 days or refrigerate or freeze.

  - 1 part PVA glue (white or Titebond 1), 10 parts water

- Flattening Solution

  - 6 parts water, 3 parts isopropyl alcohol, 1 part glycerin

  - Borden’s GF-20

Hide Glue Notes

- Use ground hide glue.

- 250 gram is best for general woodworking.  Use 200 (194) gram for veneering.

- Pre wet glue first, cover dry glue with water, stir mixture let set for ½ to an hour before heating.

- Working glue temperature is 140 – 145 degrees F, ambient 68 degrees F

- Viscosity like pancake syrup, continuous stream for 6 – 12 inches.  Add dry glue or water to get proper viscosity.

- Finger test before use

- Extend open time

  - Apply sizing to veneer and substrate

  - Heat substrate

  - Use thinner viscosity glue

- Dispose after 5 days – refrigerate or use freezing technique

- Demonstration glue pot used – Sunbeam  “Hot Pot Express” @ Target or Meijer, $13

PVA Notes

- Wait at least 1 hour after applying glue to veneer and substrate or tack free before heating.  Recommend veneering soon after glue dries

- White Glue

  - No time limit from glue application till heating

  - Iron Setting:  180 deg – Delicate setting

- Yellow Glue (Titebond 1)

  - Use within one week after glue application

  - Iron Setting:  250 deg – Between Delicate and Wool setting

- Yellow Glue (Titebond 2, Waterproof)

  - Use within three days after glue application

  - Iron Setting: 350 deg - Wool to Cotton

- “Heat Lock specialty glue – minimize veneer creep

- Recommend checking iron temperatures with a thermometer rather than using fabric settings.